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Bone Dry Products, Inc.	September 2026
9009 58th Place
Kenosha, WI 53144
Phone: 262-694-9748
E-mail: info@bonedryproducts.com
Website: http://www.bonedryproducts.com

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice.

The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all Specifier Notes when editing this section.

Brackets [__] indicate options in text to be filled in or deleted by the author; they should NOT be visible in final document.

Section numbers and titles are from MasterFormat 2018 Edition.

Please remove references to the manufacturer and preparer of this guide specification found in the header/footer.

NOTE:  Because Bone Dry can be applied during the concrete pour or prior to installation of flooring we have provided two specification sections under which to include this valuable data.  It is the specifier’s option to select the most appropriate location for his/her project.


SECTION 03 54 00
CAST UNDERLAYMENT
OR
SECTION 07 1616
CRYSTALLINE WATERPROOFING
OR
SECTION 09 05 61.13 
MOISTURE VAPOR EMISSION CONTROL
PART 1  GENERAL
1.01	SECTION INCLUDES
A.	Concrete sealers
1.02	RELATED REQUIREMENTS
A.	Section 03 30 00 – Cast-In-Place Concrete:  
B.	Section 03 53 00 – Concrete Topping
C.	Division 09 – Finishes; Flooring Sections
[bookmark: _Hlk45895175]1.03	REFERENCE STANDARDS
A.	ASTM C157 / C157M - Standard Test Method for Length Change of Hardened Hydraulic-Cement Mortar and Concrete.
B.	ASTM C39 / C39M - 18 - Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens.
C.	ASTM C1543 - Standard Test Method for Determining the Penetration of Chloride Ion into Concrete by Ponding.
D.	ASTM C666 / C666M - Standard Test Method for Resistance of Concrete to Rapid Freezing and Thawing.
E.	ASTM C672 / C672M - Standard Test Method for Scaling Resistance of Concrete Surfaces Exposed to Deicing Chemicals.
F.	ASTM D7234 - Standard Test Method for Pull-Off Adhesion Strength of Coatings on Concrete Using Portable Pull-Off Adhesion Testers.
G.	ASTM D1653 - 13 - Standard Test Methods for Water Vapor Transmission of Organic Coating Films.
H.	ASTM E96 / E96M - 16 - Standard Test Methods for Water Vapor Transmission of Materials.
I.	ASTM F2170 - 19 - Standard Test Method for Determining Relative Humidity in Concrete Floor Slabs Using in situ Probes.
J.	ASTM F1869 - 16a - Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride.
K.	ASTM E1643-11 - Standard Practice for Selection, Design, Installation, and Inspection of Water Vapor Retarders Used in Contact with Earth or Granular Fill Under Concrete Slabs.
L.	ACI 302.2R-06 - Guide for Concrete Slabs that Receive Moisture-Sensitive Flooring Materials.
M.	ASTM F710-17 - Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring.
1.04		ADMINISTRATIVE REQUIREMENTS
*********************
For warranted jobs, Contractor MUST receive approval of flooring adhesive by Bone Dry Products.
********************* 
A.	Coordinate with flooring sections for make, type and application method of adhesive and verify compatibility with sealer manufacturer.
B.	Receive approval of sealer manufacturer if installation of finish flooring will be within 14 days of concrete placement.
C.	Adhesives applied directly to sealed concrete: Provide trowel-applied or roller-applied adhesives suitable for installation over non-porous surfaces, applied in accordance with adhesive manufacturer’s specifications for non-porous substrates. Exception: Not required where sealer was applied during or shortly after concrete pour.
1.05	SUBMITTALS
A.	See Section 01 30 00 - Administrative Requirements, for submittal procedures.
B.	Product Data:  Provide manufacturer’s product literature [and testing data], listing applications and limitations.
C.	Warranty Documentation:  Submit manufacturer warranty and ensure that forms have been completed in Owner's name and registered with manufacturer.
D.	Specimen Warranty.
1.06	QUALITY ASSURANCE
A.	Manufacturer Qualifications:  Company specializing in manufacturing products specified in this section, with at least three years of [documented] experience.
B.	Installer Qualifications:  Company specializing in performing work of the type specified and with at least three years of experience.
1.07	DELIVERY, STORAGE, AND HANDLING
A.	Deliver materials to project site in original, unopened containers.
B.	Store materials in protected area not subject to freezing between 40° F (4° C) and 90° F (32° C)
C.	Store closed containers in well ventilated space.
D.	Wear protective clothing, gloves and eyewear when applying.
E.	Wear NIOSH approved respirator when handling.
1.08	FIELD CONDITIONS
A.	Ambient Conditions:  Do not install sealer when concrete is less than 40° F (4° C), or more than 90° F (32° C) for a minimum of 24 hours before or after application.
1.09	WARRANTY
A.	See Section 01 78 00 - Closeout Submittals, for additional warranty requirements.
B.	Provide manufacturer’s project-specific 25 year warranty, including material and labor to remove and replace cementitious top coating, adhesive, and finished surfaces, for damage due to concrete moisture, bonding, or pH related issues.
PART 2  PRODUCTS
2.01	MANUFACTURERS 
A.	Bone Dry Products, Inc.; Bone Dry Pro:  www.bonedryproducts.com.
B.	Substitutions:  [[Not Allowed][See Section [01 60 00 - Product Requirements][01 25 00 – Substitution Procedures]].
2.02	PERFORMANCE REQUIREMENTS
A.	Penetrating Concrete Sealer Performance (based on 4,500 psi concrete test slab results): 
1. Relative Humidity (RH), ASTM F2170: Up to 100%.
2. Moisture Vapor Emission Rate (MVER), ASTM F1869: Up to 25 lbs. / 1,000 sq. ft. per 24 hours.
3. Neutralizes elevated pH levels in concrete.
4. Curing: Functions as a curing compound; used standalone, a separate curing compound is not required.
5. Length Change, ASTM C157: 40% improvement (-0.021).
6. Freeze-Thaw Resistance, ASTM C666: Durability factor of 98.
7. Chloride Penetration, ASTM C1543: 0.168% at 0.5 inch.
8. Compressive Strength, ASTM C39: 30% improvement from control.
9. Salt Scaling, ASTM C672: 25 cycles, very slight scaling.
10. Adhesion Pull Test, ASTM D7234: 650 psi.
2.03	MATERIAL
A.	Concrete Sealer: 
1.	Composition:  Water-based silicate penetrating compound.
2.	VOC Content:  EPA Method 24; Zero VOC’s.
3.	Finish: Transparent, no sheen.
2.04	ACCESSORIES
A.	Surface Preparation:  Etch-A-Crete by Bone Dry Products, Inc. 
B.	Leveling Surface:  Concrete-based material, gypsum-based products are not allowed.
PART 3  EXECUTION
3.01	PREPARATION
A.	Existing Concrete with Surface Coatings: Provide clean porous surface by:
1. Mechanically profiling surface by diamond grinding or shot blasting surface to CSP 2 minimum.
2. Apply minimum 1/8-inch cementitious topping compound over profiled surfaces. 
B.	New Concrete with no Surface Coatings:
1. Remove construction residues and debris, including dust, paint overspray, and drywall compound, from slab surface by scraping, buffing, or broom sweeping.
2. Verify absorptivity with water droplet test: Water droplets must penetrate within 2-3 minutes; if not, etch or profile surface.
a. Apply surface preparation (Etch-A-Crete) per manufacturer’s instructions, or
b. Mechanically profile surface by diamond grinding or shot blasting surface.
C.	Verify that cracks (excluding expansion joints) exhibiting visible gaps are filled and troweled flush with cementitious patching compound.
D.	Trenches: Extend and feather cementitious patching material minimum 4 inches beyond saw cuts onto adjacent concrete substrate, prior to application of sealer.
E.	Protect surrounding finish surfaces within at least 2 feet from overspray of sealer.
F.	Ensure that areas to receive sealer are well ventilated.
G.	For newly placed concrete slabs, install vapor retarder in direct contact with underside of slab per ASTM E1643-11, ACI 302.2R-06, and ASTM F710-17.
3.02	INSTALLATION
 A.	Install in accordance with manufacturer's instructions.
1.	Contact manufacturer for approval if finished flooring will be installed within 14 days of concrete placement.
2.	Separate curing compound is not required after application of sealer.
3.	Apply sealer using pump or battery-powered sprayer equipped with wide fan tip.
*************** 
Edit the following paragraphs to project requirements.
***************
[bookmark: _Hlk45895731]B. New Concrete Applications:
1. Apply sealer in manageable sections of 1,000 to 1,500 sq ft.
2. Apply first coat of sealer uniformly to achieve saturated, lightly opaque appearance.
3. Allow to penetrate for 3-5 minutes, not exceeding 10 minutes.
4. Apply second coat while first is still wet, and only to areas where sealer has penetrated and texture of concrete is apparent.
5. Allow sealer to dry for 6 hours minimum; recommend 12 hours or overnight for full curing.
[bookmark: _Hlk45895758]C.	Application At Time of Concrete Pour Applications For Burnished Finish:
1. Consult manufacturer for application procedure where slab will be heavily burnished to a mirror-like or polished finish.
2. Allow slab to achieve sufficient hardness to support foot traffic without surface indentation.
3. Apply single heavy coat of sealer by spray at manufacturer’s recommended rate, ensuring 50 percent overlap between passes; trowel as needed to achieve desired finish.
D.	Application At Time of Concrete Pour Applications For Non-Burnished Finish:
1. Do not burnish concrete when troweling.
2. Allow slab to achieve sufficient hardness to support foot traffic, without surface indentation, after final troweling.
3. Apply single heavy coat of sealer by spray at manufacturer’s recommended rate, ensuring 50 percent overlap between passes.
4. Allow sealer to dry for 6 hours minimum.
5. Foot traffic is permitted once slab is dry to the touch.
	E.	Existing Concrete with Prior Coating Applications:
1. Sealer must be applied after leveling coat of concrete is applied to shot blasted surfaces.
2. Apply sealer at manufacturer’s recommended rate; allow sealer to absorb for 3-5 minutes, not exceeding 10 minutes.
3. Apply second coat to areas while first coat is still wet but has penetrated concrete.
4. Allow sealer to dry for 6 hours minimum.
5. Remove loose dry product by lightly scraping concrete.
	F.	When Applying to Receive Resin Based Systems:
1. Apply over surfaces with CSP 3 profile.
2. Use 100% solids epoxy, urethane, polyaspartic, or other resin systems.
3. No cement-based top coating required.
	G.	Coverage Rates:
1. Broom-finished, troweled, or mechanically profiled: 300-340 sq ft/gal.
2. Heavily burnished, polished, or Etch-a-Crete-treated: 350-400 sq ft/gal.
3. Intensive burnishing or polishing: Up to 500 sq ft/gal.
3.03	CLEANING
A.	Vacuum loose particles prior to applying approved flooring adhesives.
B.	See Section 01 74 19 - Construction Waste Management and Disposal, for disposal of containers.
3.04	PROTECTION
A.	Do not permit traffic on floor surface until fully dried.
END OF SECTION
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