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Bone Dry Products, Inc.	October 2026
9009 58th Place
Kenosha, WI 53144
Phone: 262-694-9748
E-mail: info@bonedryproducts.com
Website: http://www.bonedryproducts.com

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice.

The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all Specifier Notes when editing this section.

Brackets [__] indicate options in text to be filled in or deleted by the author; they should NOT be visible in final document.

Section numbers and titles are from MasterFormat 2018 Edition.

Please remove references to the manufacturer and preparer of this guide specification found in the header/footer.

NOTE:  Because Bone Dry can be applied during the concrete pour or prior to installation of flooring we have provided two specification sections under which to include this valuable data.  It is the specifier’s option to select the most appropriate location for his/her project.


SECTION 03 54 00
CAST UNDERLAYMENT
OR
SECTION 07 1616
CRYSTALLINE WATERPROOFING
OR
SECTION 09 05 61.13
MOISTURE VAPOR EMISSION CONTROL
PART 1  GENERAL
1.01	SECTION INCLUDES
A.	Concrete sealers
1.02	RELATED REQUIREMENTS
*************** 
Edit the following paragraphs to project requirements.
***************
A.	Section 03 30 00 – Cast-In-Place Concrete:  
B.	Section 03 53 00 – Concrete Topping
C.	Division 09 – Finishes; Flooring Sections
[bookmark: _Hlk45895175]1.03	REFERENCE STANDARDS  --  VERIFY
A.	Not Used.
1.04	ADMINISTRATIVE REQUIREMENTS
A.	Coordinate with flooring sections for make, type and application method of adhesive and verify compatibility with sealer manufacturer.
B.	Receive approval of sealer manufacturer if installation of finish flooring will be less than 14 days after concrete pour.
1.05	SUBMITTALS
A.	See Section 01 30 00 - Administrative Requirements, for submittal procedures.
[bookmark: _Hlk45900752]B.	Product Data:  Provide manufacturer’s product literature [and testing data], listing applications and limitations.
C.	Specimen Warranty.
1.06	QUALITY ASSURANCE
A.	Manufacturer Qualifications:  Company specializing in manufacturing products specified in this section, with at least three years of [documented] experience.
B.	Installer Qualifications:  Company specializing in performing work of the type specified and with at least three years of experience.
1.07	DELIVERY, STORAGE, AND HANDLING
A.	Deliver materials to project site in original, unopened containers.
B.	Store materials in protected area at temperatures above freezing and below 90° F (32° C); shelf life is 2 years.
C.	Store closed containers in well ventilated space.
D.	Wear protective clothing, gloves and eyewear when applying.
E.	Wear NIOSH approved respirator when handling.
1.08	FIELD CONDITIONS
A.	Ambient Conditions:  Do not install sealer when concrete is less than 35° F (2° C), or more than 95° F (35° C) for a minimum of 24 hours before or after application.
1.09	WARRANTY
A.	See Section 01 78 00 - Closeout Submittals, for additional warranty requirements.
B.	Provide manufacturer’s limited warranty stating that the product is free of defects and covering replacement of the Bone Dry product only in the event of a claim on the product.
PART 2  PRODUCTS
2.01	MANUFACTURERS 
A.	Bone Dry Products, Inc.; Bone Dry Original:  www.bonedryproducts.com.
B.	Substitutions:  [[Not Allowed][See Section [01 60 00 - Product Requirements][01 25 00 – Substitution Procedures]].
[bookmark: _Hlk45895394]2.02	PERFORMANCE REQUIREMENTS
A.	Protects finished flooring, coatings, and adhesives from concrete slabs containing up to 100 percent relative humidity (RH), calcium chloride readings reaching 25 lbs, and neutralizes high pH in concrete.
2.03	MATERIAL
A.	Concrete Sealer: 
1.	Composition:  Water-based silicate penetrating compound.
2.	Finish: Transparent, no sheen.
2.04	ACCESSORIES
A.	Surface Preparation:  Etch-A-Crete by Bone Dry Products, Inc. 
B.	Primer:  Bone Dry Primer by Bone Dry Products, Inc.
C.	Leveling, Patch, and Skim Coat Products:  Cement-based material with minimum compressive strength of 4,000 psi at 28 days; gypsum-based products, including Gyp-Crete, are not allowed.
PART 3  EXECUTION
3.01	PREPARATION
[bookmark: _Hlk45900853][bookmark: _Hlk45895474]A.	Existing Concrete with Surface Coatings: Provide clean porous surface by:
1.	Mechanically profiling surface by diamond grinding or shot blasting to a minimum concrete surface profile of CSP 2; where an epoxy, urethane, polyaspartic, or other resin system is to be applied, profile to CSP 3.
2.	Concrete with known moisture problems or over 10 years of age must receive a top coating of a cement-based product after being profiled to CSP 2; contact manufacturer for exceptions to this requirement. Where an epoxy, urethane, polyaspartic, or other resin system is to be applied, a cement-based top coating is not required.
B.	Thoroughly clean floor, of dust, paint, gypsum board compound, and other materials that interfere with complete coverage of sealer.
C.	If slab has no existing surface coatings but has received a heavily burnished (mirror-like) or polished finish either:
1.	Apply surface preparation (Etch-A-Crete) per manufacturer’s instructions, or
2.	Mechanically profile surface by diamond grinding or shot blasting surface.
D.	If sealer will be applied on porous, non-painted, cement-based material (concrete block, gunite, or shotcrete) coat surface with primer as recommended by manufacturer.
1.	Clean surfaces of oil, grease and acidic conditions prior to applying primer.
[bookmark: _Hlk45900868]E.	Verify that cracks (excluding expansion or control joints) with visible gaps are filled and floated over with cement.
[bookmark: _Hlk49172492]1.	Cover trench saw cuts with cement-based coating prior to application of sealer.
F.	Protect surrounding finish surfaces within at least 24 inches from overspray of sealer.
G.	Ensure that areas to receive sealer are well ventilated.
H.	Do not apply sealer to existing decorative exposed aggregate or stained concrete surfaces; discoloration may occur.
3.02	INSTALLATION
A.	Install in accordance with manufacturer's instructions.
[bookmark: _Hlk49172151]1.	Contact manufacturer for approval if finished flooring will be installed less than 14 days after the concrete pour.
[bookmark: _Hlk49174135]2.	Curing compound is not required after application of sealer.
3.	Spread rates:  Broom-troweled surfaces, 200 to 250 sq. ft. per gallon; mechanically troweled surfaces, 300 to 350 sq. ft. per gallon; heavily burnished or polished surfaces where slab pores are opened with Etch-A-Crete, 350 to 450 sq. ft. per gallon.
4.	Adhesives applied directly to the sealed concrete surface shall be applied per specifications for a non-porous substrate, except where sealer was applied during the concrete pour.
*************** 
Edit the following paragraphs to project requirements.
***************
B.	Newly Cured Concrete Applications:
1.	Apply first coat of sealer so that the slab receives a wet to slightly cloudy appearance; after completing a section, let the area sit for no more than 10 minutes before applying second coat.
2.	Apply second coat only to areas where sealer has penetrated and texture of concrete has become visible.
a.	Use broom or brush to spread pooled sealer.
3.	Allow sealer to dry for 6 hours minimum.
[bookmark: _Hlk45901010]C.	Application At Time of Concrete Pour:
1.	Do not apply cure and seal products or water during curing.
2.	Apply sealer once concrete surface is hard enough to walk on without indentations after final troweling.
3.	Apply one coat of sealer with a 50 percent overlap at the specified spread rate; only one coat is required.
4.	Allow sealer to dry for 6 hours minimum.
5.	When applied at the time of the pour, apply curing or insulating blankets after the sealer is dry to the touch; if time constraints require the blankets to be placed while the sealer is still wet, this is acceptable and will not adversely affect the sealer’s performance.
D.	Existing Concrete with Prior Coating Applications:
1.	Apply sealer after floor leveling and skim coating of the profiled surface, and any sanding of the leveled or skim-coated surface, are complete; minor patching and skim coating may also be completed after sealer is applied.
2.	Apply one coat of sealer at the specified spread rate so that the slab receives a wet to slightly cloudy appearance; after completing a section, let the area sit for no more than 10 minutes before applying second coat.
3.	Apply second coat only to areas where sealer has penetrated and texture of concrete has become visible.
4.	Allow sealer to dry for 6 hours minimum.
5.	Remove loose dry product by lightly scraping concrete.
3.03	CLEANING
A.	Vacuum loose particles prior to applying approved flooring adhesives.
B.	See Section 01 74 19 - Construction Waste Management and Disposal, for disposal of containers.
3.04	PROTECTION
A.	Do not permit traffic on floor surface until fully dried.
END OF SECTION
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