SECTION 03 35 00

CONCRETE FINISHING

PENETRATING LITHIUM SILICATE / NANO SILICA CONCRETE DENSIFIER

Basis of Design: Bone Dry Li 200 Logistics — Bone Dry Products, Inc.

Revised October 2026

SPECIFIER NOTE: This guide specification is written in CSI 3-part format for incorporation into project manuals. Edit bracketed selections and delete this note before issue. Coordinate with Section 03 30 00 for concrete placement and finishing tolerances. Li 200 Logistics assists in evenly curing the slab in the same manner as a curing compound; a separate curing compound is not necessary. Where a curing compound is nonetheless required, apply it after Li 200 Logistics.

PART 1 — GENERAL

1.1  SUMMARY

A. Section Includes: Penetrating, water-based, high-solid-content lithium silicate and nano silica liquid densifier for exposed interior and exterior concrete surfaces in high-traffic and heavy-traffic environments.

B. Related Sections:

1. Section 03 30 00 — Cast-in-Place Concrete.

2. Section 03 35 43 — Polished Concrete Finishing.

3. Section 03 39 00 — Concrete Curing.

4. Section 03 05 59 — Post-Applied Concrete Treatments (Concrete Densifiers).

1.2  REFERENCES

A. ASTM International:

1. ASTM C39 — Compressive Strength of Cylindrical Concrete Specimens.

2. ASTM C157 — Length Change of Hardened Hydraulic-Cement Mortar and Concrete.

3. ASTM C666 — Resistance of Concrete to Rapid Freezing and Thawing.

4. ASTM C672 — Scaling Resistance of Concrete Surfaces Exposed to Deicing Chemicals.

5. ASTM C1543 — Determining the Penetration of Chloride Ion into Concrete by Ponding.

6. ASTM D4060 — Abrasion Resistance of Organic Coatings by the Taber Abraser.

7. ASTM C1583 — Tensile Strength of Concrete Surfaces and the Bond Strength or Tensile Strength of Concrete Repair and Overlay Materials by Direct Tension (Pull-off Method).

B. DIN 1048 — Testing Concrete: Water Penetration.

C. Alberta Transportation B388 — Concrete Sealer Performance.

D. USGBC LEED Version 4, BD&C and ID&C; The WELL Building Standard; ANSI/GBI 01 Green Building Assessment Protocol.

1.3  SUBMITTALS

A. Product Data: Manufacturer's specifications and technical data including product description, attributes, spread rates, application instructions, and storage requirements.

B. Test Reports: Test data demonstrating compliance with performance criteria specified in Article 2.3.

C. Safety Data Sheets (SDS).

D. Warranty: Sample copy of manufacturer's 25-year limited product warranty.

1.4  QUALITY ASSURANCE

A. Manufacturer Qualifications: Company specializing in the manufacture of penetrating concrete densifiers and moisture mitigation products.

B. Field Sample (Mockup): Apply densifier to a minimum 100 sq. ft. test area of representative substrate to confirm spread rate, appearance, and drying time. Approved test area may remain as part of the Work.

1.5  DELIVERY, STORAGE, AND HANDLING

A. Deliver materials in original, unopened containers with manufacturer's labels intact.

B. Store in conditions above freezing (32°F) and below 90°F.

C. Shelf Life: 2 years in original sealed container.

1.6  PROJECT CONDITIONS

A. Substrate shall be clean and porous. Existing coatings shall be mechanically removed prior to application.

B. Freshly poured concrete shall be hard enough for foot traffic prior to application.

C. Protect adjacent finished surfaces from overspray; excessive overspray may discolor surfaces.

D. Application temperature: apply when ambient and surface temperatures are between 35 °F and 95 °F (2 °C and 35 °C).

1.7  WARRANTY

A. Manufacturer's Warranty: 25-year limited product warranty stating that the treated surface will remain water-resistant, dustproof, hardened, and abrasion resistant for 25 years from the application date.

PART 2 — PRODUCTS

2.1  MANUFACTURER

A. Basis of Design: Bone Dry Products, Inc.; 9009 58th Place, Kenosha, WI 53144; Phone: 262-694-9748; Email: info@bonedryproducts.com; Web: bonedryproducts.com.

B. Substitutions: [Not permitted.] [Submit in accordance with Section 01 25 00 — Substitution Procedures.]

2.2  MATERIALS

A. Penetrating Densifier: Bone Dry Li 200 Logistics — high-solid-content lithium silicate and nano silica densifying solution formulated to penetrate deep into concrete and dry clear without brooming or removal after application. Product is not membrane-forming and is intended to densify exposed concrete surfaces.

B. Physical Characteristics:

1. Water based; Low VOC.

2. Suitable for interior and exterior use.

3. Breathable and UV stable.

4. Compatible with reactive and resin bond breakers.

C. Performance Attributes: Densifies and hardens concrete; eliminates dusting; improves water and stain resistance; protects against efflorescence (ASR); increases abrasion resistance; fills microcracks and increases sheen; increases compression strength; assists in evenly curing the concrete slab in the same manner as a curing compound.

2.3  PERFORMANCE CRITERIA

A. Densifier shall demonstrate the following performance when tested per the referenced standards:

| Test Method | Property | Duration / Age | Result — Li 200 Logistics |
| --- | --- | --- | --- |
| ASTM C672 | Scaling resistance (deicing chemicals) | 25 cycles | Rating 1 (Very Slight); Control: Rating 3 (Moderate) |
| ASTM C672 | Scaling resistance (deicing chemicals) | 50 cycles | Rating 2 (Slight); Control: Rating 5 (Severe) |
| Alberta B388 | Water loss | — | 79% reduction |
| Alberta B388 | Waterproofing performance | — | 70% increase |
| ASTM C39 | Compressive strength | 4 days | 2% increase over control |
| ASTM C39 | Compressive strength | 7 days | 12% increase over control |
| ASTM C39 | Compressive strength | 14 days | 16% increase over control |
| ASTM C39 | Compressive strength | 28 days | 30% increase over control |
| DIN 1048 | Water penetration | — | 23% improvement |
| ASTM C157 | Length change (drying shrinkage) | — | 40% reduction |
| ASTM C666 | Freeze/thaw resistance | — | 48% improvement |
| ASTM C1583 | Pull-off strength | 7 days | 533 psi |
| ASTM C1543 | Chloride ion penetration | at 1 in. depth | 0.064% |
| ASTM D4060 | Taber abrasion resistance | — | 29% increase |

2.4  SUSTAINABILITY

A. Product supports USGBC LEED Version 4 (BD&C, ID&C), The WELL Building Standard, and ANSI/GBI 01 Green Building Assessment Protocol.

PART 3 — EXECUTION

3.1  EXAMINATION

A. Verify substrate is clean, porous, and free of coatings, curing compounds, sealers, and contaminants that inhibit penetration. Mechanically remove existing coatings.

B. For freshly poured concrete, verify slab is hard enough for foot traffic prior to application.

C. When applied at the time of the pour, apply curing or insulating blankets after the sealer is dry to the touch; if time constraints require the blankets to be placed while the sealer is still wet, this is acceptable and will not adversely affect the sealer’s performance.

D. Do not proceed until unsatisfactory conditions have been corrected.

3.2  PREPARATION

A. Protect adjacent finished surfaces from overspray.

3.3  APPLICATION

A. Equipment: Apply using a pump or battery-powered sprayer with a cone or wide fan spray tip.

B. Apply by fully wetting the concrete slab; avoid puddling. Slab shall remain wet for 10 to 15 minutes.

C. Allow slab to become dry to the touch (typically 2 to 3 hours) prior to resuming traffic.

D. If dust appears on the surface due to heavy puddling, broom sweep once dry.

E. A separate curing compound is not necessary. Where a curing compound is required by other Sections, apply it after application of Li 200 Logistics.

3.4  APPLICATION RATES

A. Hard troweled surfaces: 400 to 800 sq. ft. per gallon.

B. Broom finished concrete: 200 to 400 sq. ft. per gallon.

C. Actual coverage varies with surface texture and porosity; confirm with field sample per Article 1.4.

3.5  FIELD QUALITY CONTROL

A. Verify application rate by monitoring material usage against treated area; adjust application to maintain specified spread rates.

B. Inspect treated surfaces for uniform coverage and complete absorption of visible puddling prior to demobilization.

3.6  CLEANING

A. Clean sprayers, brooms, and application equipment with water immediately after use.

B. Remove overspray from adjacent finished surfaces immediately.

3.7  PROTECTION

A. Protect treated surfaces from traffic until dry to the touch (typically 2 to 3 hours after application).

END OF SECTION 03 35 00